Image analysis

You have two sets of SEM images acquired from different samples (black and green) that you need to analyze. The goal is to get a particle size distribution from the images, as well as calculate airborne concentrations based on sampled volume, analyzed area, and effective sample collection area. In addition, you need to assess the aspect ratio and other shape parameters for the particle distribution.

Tasks

- Load an image and crop the information bar at the bottom

- Use a simple global threshold to binarize the image – consider using a threshold determined automatically – or explore alternative segmentation options

- Obtain individual particle metrics of size, shape, and other parameters for all recognized particles

- Extend the script to loop through images from one sample and obtain a sample-wide particle size distribution.

- Determine airborne concentrations by extracting sampling time and flowrate for each of the two samples. This can be determined from the .txt partector dataset. The TEM column denotes when the instrument is sampling (1 = sampling, 0 = not sampling). The black sample was collected first. The average flow of the instrument can be determined from the flow column while actively sampling.

- Once the average flow and sampling time are known, determine the airborne concentration. To do this, you need to know that the total sample area is 7.302 mm2 and that each image has a pixel resolution of 8.44 nm/pixel. Now calculate the total imaged area, and extrapolate the determined number concentration to the full sample area, and then to airborne concentration based on sampling time and flow.